

	Inspection Item
	Premium Grade
(Requirement)
	First Grade
(Requirement)
	Qualified Grade
(Requirement)
	Test Result

	Appearance
	White flaky or crystalline powder
	White flaky or crystalline powder slightly with other hues
	/
	Qualified

	Melt Color(Color Number)≤
	20
	50
	100
	15

	Heat Stabilized Color(Color Number)≤
	50
	150
	-
	25

	Sulfuric Acid Color Number≤
	40
	100
	150
	20

	Crystallization Point/℃≥
	130.5
	130.3
	130.0
	131

	Purity of Phthalic Anhydride %≥
	99.50
	99.50
	99.50
	99.956

	Free Acid (Mass Fraction)%≤
	0.20
	0.30
	0.50
	0.010




