| Inspection Item | Premium Grade (Requirement) | First Grade (Requirement) | Qualified Grade (Requirement) | Test Result |
| --- | --- | --- | --- | --- |
| Appearance | White flaky or crystalline powder | White flaky or crystalline powder slightly with other hues | / | Qualified |
| Melt Color(Color Number)≤ | 20 | 50 | 100 | 15 |
| Heat Stabilized Color(Color Number)≤ | 50 | 150 | - | 25 |
| Sulfuric Acid Color Number≤ | 40 | 100 | 150 | 20 |
| Crystallization Point/℃≥ | 130.5 | 130.3 | 130.0 | 131 |
| Purity of Phthalic Anhydride %≥ | 99.50 | 99.50 | 99.50 | 99.956 |
| Free Acid (Mass Fraction)%≤ | 0.20 | 0.30 | 0.50 | 0.010 |